Cyclic Large Deflection Testing of Shaft Bridges

Part II: Analytical Studies

PRINCIPAL INVESTIGATOR

John W. Wallace

University of California, Los Angeles

CO-PRINCIPAL INVESTIGATORS

Patrick J. Fox and Jonathan P. Stewart
University of California, Los Angeles

SUPPORTED GRADUATE STUDENTS

Kerop Janoyan

Clarkson University, Potsdam, NY

Tong Qiu

University of California, Los Angeles

Sandrine P. Lermitte

University of California, Los Angeles

A report on research conducted under Grant No. 59A0183 

from the California Department of Transportation

Department of Civil and Environmental Engineering

University of California, Los Angeles

December 2001

CONTENTS

CONTENTS
iii

LIST OF FIGURES
vii

LIST OF TABLES
xv

LIST OF SYMBOLS
xvii

ACKNOWLEDGMENTS
xxv

EXECUTIVE SUMMARY
xxvii

1
INTRODUCTION
1


1.1
Introduction
1


1.2
Objectives and Scope
1


1.3
Organization
1

2
2-D FINITE ELEMENT MODEL OF A CAST IN DRILLED SHAFT 

BRIDGE COLUMN 
3


2.1
Generation of the Model
3



2.1.1
Material properties used for the shaft/column model
3




2.1.1.1
Analytical modeling of reinforcement stress-strain behavior
4




2.1.1.2
Analytical modeling of reinforced concrete stress-strain behavior
4



2.1.2
Two-dimensional fiber model
6



2.1.3
Soil model
6



2.1.4
Gravity load and mass distribution
7


2.2
Static Analysis
7



2.2.1
Moment curvature analysis 
8



2.2.2
Nonlinear static pushover using API p-y curves
9




2.2.2.1
Global response of the analytical model using API p-y curves
10




2.2.2.2
Local response of the analytical model using API p-y curves
10



2.2.3
Parametric sensitivity study on the model
11




2.2.3.1
Sensitivity study on vertical distribution of soil springs
12




2.2.3.2
Sensitivity study on the soil properties
14




2.2.3.3
Sensitivity study on influence of soil at large depth
16




2.2.3.4
Sensitivity study on the effect of additional moment

at ground line due to the system loading
19


2.3
Recommendations Based on the Sensitivity Studies
20

3
NONLINEAR PUSHOVER ANALYSIS: COMPARISON 


BETWEEN ANALYTICAL MODELS RESULTS AND TEST RESULTS
37


3.1
API p-y Curves
37



3.1.1
API p-y curves generation
37



3.1.2
Shaft/column response
38


3.2
Experimental p-y Curves
39



3.2.1
Experimental p-y curves generation
39



3.2.2
Shaft/column response
40


3.3
Experimental Test Results
42


3.4
Comparison of Analytical Results with Experimental Results
44


3.5
Summary
47

4
CYCLIC ANALYSES
63


4.1
Cyclic Analysis – No Gapping
63



4.1.1
Cyclic response – API p-y curves
64



4.1.2
Cyclic response – Experimental p-y curves
65



4.1.3
Cyclic response – Local behavior
66


4.2
Effect of Gapping
70



4.2.1
Background on gapping effects
70



4.2.2
Existing models
71



4.2.3
Radiation damping
75



4.2.4
Model validation
76



4.2.5
Model evaluation
77



4.2.6
Simplified model
81




4.2.6.1
Simplified p-y gap element: Development and assessment
82




4.2.6.2
Proposed simplified model
83




4.2.6.3
Drag Model
86


4.3
Cyclic Response Analyses – Gap Element Model
87



4.3.1
Cyclic response analyses - 20% Drag
88



4.3.2
Cyclic response analyses - 50% Drag
89



4.3.3
Cyclic response analyses - 80% Drag
90



4.3.4
Results Comparison – 20%, 50% and 80% Drag
92


4.4
Specific Study of Soil Springs Behavior
96



4.4.1
Comparison of spring behavior 





for 20% and 80% drag force models
96



4.4.2
Spring behavior for 50% drag force model
97

5
PREDICTION FOR 2 FT DIAMETER SHAFT/COLUMN 
121


5.1
Analytical Model
121



5.1.1
Specimen description
121



5.1.2
Material properties
122



5.1.3
Two-dimensional fiber model
123



5.1.4
Soil model
124


5.2
Static Analyses of 2 ft (0.6 m) Shaft/Column
124


5.3
Cyclic Analyses of 2 ft (0.6 m) Shaft/Column
126



5.3.1
Cyclic analysis – No gapping
127



5.3.2
Cyclic analysis – Gapping included
127

6
SITE DESCRIPTION AND SELECTION OF MATERIAL PROPERTIES
139


6.1
Investigations Performed
139


6.2
Soil Profile
139


6.3
In Situ Testing Program
140


6.4
Laboratory Testing Program
143


6.5
Selection of Soil Properties for ABAQUS Simulations
148


6.6
Selection of Reinforced Concrete Properties for ABAQUS Simulations
154

7
FINITE ELEMENT SIMULATIONS FOR 6 FT. AND 2 FT


DIAMETER SHAFTS
163


7.1
Model Description
163



7.1.1
Types of Elements for Soil and Shaft
163



7.1.2
Size of Finite Element Mesh
165


7.2
Model Symmetry
170


7.3
Initial Soil Effective Stress Condition
170


7.4
ABAQUS Simulations for 6 ft. Diameter Shaft
172


7.5
ABAQUS Predictions for 2 ft. Diameter Shaft
184


7.6
Effect of Shaft Diameter on Results of ABAQUS Numerical Simulations
190

8
CONCLUSIONS 
195


8.1
Research Findings
196



8.1.1
Findings: P-y studies
196




8.1.1.1
Model assessment 
196




8.1.1.2
Soil-structure-interaction-effect – Static analyses 
197




8.1.1.3
Soil-structure-interaction-effect – Cyclic analyses 
198



8.1.2
Findings: ABAQUS studies
200


8.2
Recommendations for Future Work
202



8.2.1
P-y studies
202



8.2.2
3D Finite element studies
203

REFERENCES: 
205

APPENDICES: 
213


Appendix 1:
Sensitivity of soil spring spacing for 4 ft and 8 ft shaft/column
213


Appendix.2:
Opensees input file
219


Appendix 3:
Opensees complex gap model
237


Appendix 4:
Opensees simple gap model
253

LIST OF FIGURES

2.1 
Stress-strain curve for modeled transverse reinforcing steel
22

2.2 
Modified Kent-Park stress-strain model
23

2.3 
Stress-strain curve for modeled reinforced concrete
23

2.4 
Cross-section of the fiber model
24

2.5 
Moment-curvature diagram
24

2.6 
Sensitivity study on spring locations
25

2.7 
Nonlinear pushover analyses at top shaft/column
26

2.8 
Nonlinear pushover analyses at ground line
26

2.9 
Displacement profile at different applied force levels 


on top of shaft/column
27

2.10 
Shear profile at different applied force levels


on top of shaft/column
27

2.11 
Moment profile at different applied force levels on top of shaft/column
28

2.12 
Curvature profile at different applied force levels on top of shaft/column
28

2.13 
Nonlinear pushover analyses at top shaft/column
29

2.14 
Nonlinear pushover analyses at ground line
29

2.15 
Displacement profile for F=300 kips applied at the top of the shaft/column
30

2.16 
Shear profile for F=300 kips applied at the top of the shaft/column
30

2.17 
Moment profile for F=300 kips applied at the top of the shaft/column
31

2.18 
Curvature profile for F=300 kips applied at the top of the shaft/column
31

2.19 Nonlinear pushover at top shaft/column (both p and y are factored by a constant 


factor k)
32

2.20 Curvature profile at yield displacement level (both p and y are factored by a 


constant factor k)
32

2.21 
Nonlinear pushover at top shaft/column (only y is factored by k)
33

2.22 
Curvature profile at yield displacement level (only y is factored by k)
33

2.23 
Height effect on a fixed-base cantilever structural response
34

2.24 
Effect of soil model at large depth
34

2.25 Nonlinear pushover analyses at ground line for shaft/columns models extending 


48 ft below ground, and H above grade
35

2.26 Curvature profile at yield displacement level for shaft/column models extending 


48 ft below ground, and H above grade
35

3.1 
API p-y curves for soil considered at depth between 1 ft and 48 ft
49

3.2 
Trilinear API p-y approximation
50

3.3 
Nonlinear pushover analysis at top shaft/column using API p-y curves
51

3.4 
Nonlinear pushover analysis at ground line, using API p-y curves
51

3.5 Curvature profile for three characteristic displacement levels (model using 


API p-y curves)
52

3.6 Displacement profile for three characteristic displacement levels (model using 


API p-y curves)
52

3.7 
Experimental p-y curves at 1, 2, 4, and 5 ft below ground
53

3.8 
Trilinear approximation for experimental p-y curves
54

3.9 Nonlinear pushover analysis at top of the shaft/column, using experimental 


p-y Curves
55

3.10 
Nonlinear pushover analysis at ground line, using experimental p-y curves
55

3.11
Curvature profile for three characteristic displacement levels (model using 


experimental p-y curves)
56

3.12
Displacement profile for three characteristic displacement levels 


(model using experimental p-y curves)
56

3.13 
Trilinear approximation of the test results envelope
57

3.14 
Envelope of the test results at the top of the shaft/column
57

3.15 
Envelope of the test results at ground-line level
58

3.16 
Curvature profile derived from experimental data
58

3.17 
Displacement profile derived from experimental data
59

3.18 
Comparison of analytical models versus in situ results at top shaft/column
59

3.19 
Comparison of analytical models versus in situ results at ground line
60

3.20 
Comparison of analytical models versus in situ results at yield level
60

3.21 
Plastic length versus displacement level
61

3.22 
Comparison of analytical model versus in situ results, at yield level
61

3.23 
Comparison of analytical model versus in situ results
62

4.1 
Shaft-soil gapping during the 1994 Northridge Earthquake
98

4.2 
Effect of cyclic loading on p-y curves based on Reese equation (1972)
98

4.3 
Cyclic response, model using API p-y curves
99

4.4 Comparison of cyclic response at three level displacements 


(9, 40, 83 in peak shaft/column displacement)
99

4.5 
Cyclic response, model using experimental p-y curves
100

4.6
Comparison of cyclic response at three level displacements


(9, 40, 83 in peak top shaft/column displacement)
100

4.7 
Cyclic curvature profile at peak top shaft/column displacement of 9 in.
101

4.8 
Cyclic curvature profile at peak top shaft/column displacement of 40 in.
101

4.9 
Cyclic curvature at peak top shaft/column displacement of 83 in.
102

4.10 
Cyclic displacement profile at top shaft/column displacement of 9 in.
102

4.11 
Cyclic displacement profile at top shaft/column displacement of 40 in
103

4.12 
Cyclic displacement profile at top shaft/column displacement of 83 in
103

4.13 
Soil model
104

4.14 Soil model including, elastic, plastic, drag, closure and radiation damping 


effect (Boulanger et al., 1999)
105

4.15 
Radiation damping models (Wang, 1998)
106

4.16 
Plastic model
107

4.17 
Drag model
107

4.18 
Closure model
108

4.19 
Soil spring model including gap model
108

4.20 
Soil spring model proposed to incorporate gapping effect
109

4.21 
Soil spring cyclic response for different models
109

4.22 
Component of soil resistance p (Smith, 1986)
110

4.23 
Fraction of normal soil reaction p that can be attributed to normal stress
110

4.24 
Cyclic response, analytical model with 20% drag force
112

4.25 
Curvature profile, analytical model with 20% drag force
112

4.26 
Displacement profile, analytical model with 20% drag force
113

4.27
Cyclic response, analytical model with 50% drag force
113

4.28 
Curvature profile, analytical model with 50% drag force
114

4.29 
Displacement profile, analytical model with 50% drag force
114

4.30 
Cyclic response, analytical model with 80% drag force
115

4.31 
Curvature profile, analytical model with 80% drag force
115

4.32 
Displacement profile, analytical model with 80% drag force
116

4.33 Comparison between experimental results and analytical model


80% drag force
116

4.34 Comparison between experimental results and analytical model 


80% drag force
117

4.35
Comparison between experimental results and analytical model


80% drag force
117

4.36 
Spring behavior at 2 ft below ground – 20% drag model 
118

4.37 
Spring behavior at 2 ft below ground – 80% drag model 
118

4.38 
Spring behavior at 10 ft below ground – 20% drag model 
119

4.39 
Spring behavior at 10 ft below ground – 80% drag model 
119

4.40 
Spring elements participation – 50% drag force
120

4.41 
Elastic, plastic and drag element behavior
120

5.1 
Shaft/column description
129

5.2 
Moment-curvature relationship for 2 ft (0.6 m) shaft/column
129

5.3 
API and Experimental p-y curves for 2 ft shaft/column
130

5.4 
Pushover at top shaft/column
131

5.5 
Pushover at ground line
131

5.6 
Curvature profile
132

5.7 
Displacement profile
132

5.8 
Shear profile
133

5.9 
Moment profile
133

5.10 
Cyclic loading
134

5.11 
Cyclic response at top shaft/column – No gap
134

5.12 
Cyclic response at ground line – No gap
135

5.13 
Cyclic response at top shaft/column – 20% drag force
135

5.14 
Cyclic response at top shaft/column – 50% drag force
136

5.15 
Cyclic response at top shaft/column –80% drag force
136

5.16 
Curvature profile for top shaft/column displacement of 6 in.
137

6.1
Typical preboring pressuremeter curve (Briaud 1986)
144

6.2
Dial readings vs. time for consolidation test P1-5 (Δσv = 500 psf)
 146

6.3
Mohr-Coulomb failure model
149

6.4
Void ratio vs log pressure for consolidation test P1-5
150

6.5
P - ∆R/R0 curve for PMT-1 at a depth of 11 ft. 
151

6.6
Problem geometry and soil profile with upper bound E values
155

6.7
Problem geometry and soil profile with lower bound E values
156

6.8
Problem geometry and soil profile with average E values
157

6.9
Moment-curvature relationship for 6 ft. diameter shaft
159

6.10
Deformed shaft with nodes and coordinates
161

7.1
ABAQUS elements for shaft and soil
164

7.2
Side view of final mesh for 6 ft. diameter drilled shaft
166

7.3
Top view of final mesh for 6 ft. diameter drilled shaft
167

7.4
Effect of soil element order on contact pressure distribution
168

7.5
Effect of mesh diameter on contact pressure distribution
169

7.6
Dimensions of the final mesh for 6 ft. shaft simulations
169

7.7
Plane of symmetry and contact surfaces
170

7.8
Staged simulations to reproduce initial soil effective stress condition
171

7.9
Lateral load vs. lateral displacement at top of 6 ft. diameter shaft
172

7.10
p-y curves at a depth of 3 ft. for 6 ft. diameter shaft
173

7.11
p-y curves at a depth of 7.5 ft. for 6 ft. diameter shaft
174

7.12
p-y curves at a depth of 17.5 ft. for 6 ft. diameter shaft
174

7.13
Plots of curvature vs. depth at a displacement of 2 in. 


at top of 6 ft. diameter  shaft
175

7.14
Plots of curvature vs. depth at a displacement of 4 in. 


at top of 6 ft. diameter shaft
176

7.15
Plots of curvature vs. depth at a displacement of 12 in. 


at top of 6 ft. diameter  shaft
176

7.16
Plots of curvature vs. depth at a displacement of 24 in. 


at top of 6 ft. diameter shaft
177

7.17
Plots of curvature vs. depth at a displacement of 48 in. 


at top of 6 ft. diameter shaft
177

7.18
Plots of shaft displacement vs. depth at a displacement of 2 in. 


at top of 6 ft. diameter shaft
178

7.19
Plots of shaft displacement vs. depth at a displacement of 4 in. 


at top of 6 ft. diameter shaft
179

7.20
Plots of shaft displacement vs. depth at a displacement of 12 in. 


at top of 6 ft. diameter shaft
179

7.21
Plots of shaft displacement vs. depth at a displacement of 24 in. 


at top of 6 ft. diameter shaft
180

7.22
Plots of shaft displacement vs. depth at a displacement of 48 in. 


at top of 6 ft. diameter shaft
180

7.23
Gap width, shaft displacement at ground surface vs. displacement 


at top of 6 ft. diameter shaft
182

7.24
Gap depth vs. displacement at top of 6 ft. diameter shaft
183

7.25
Hinge point depth vs. displacement at top of 6 ft. diameter shaft
183

7.26
Dimensions of the final mesh for the 2 ft. shaft simulations
185

7.27
Lateral load vs. lateral displacement at top of 2 ft. diameter shaft
185

7.28
p-y curves at a depth of 3 ft. for 2 ft. diameter shaft
186

7.29
p-y curves at a depth of 7.5 ft. for 2 ft. diameter shaft
186

7.30
p-y curves at a depth of 10 ft. for 2 ft. diameter shaft
187

7.31
Plots of curvature vs. depth at different displacements 


at top of 2 ft. diameter shaft
187

7.32
Plots of shaft displacement vs. depth at different displacements  


at top of 2 ft. diameter shaft
188

7.33
Gap width at the ground surface vs. displacement 


at top of 2 ft. diameter shaft
188

7.34
Gap depth vs. displacement at top of 2 ft. diameter shaft
189

7.35
Hinge point depth vs. displacement at top of 2 ft. diameter shaft
189

7.36
Normalized displacement vs. normalized depth for 2 ft. diameter shaft
192

7.37
Normalized displacement vs. normalized depth for 6 ft. diameter shaft
192

7.38
Normalized curvature vs. normalize depth for 2 ft. diameter shaft
193

7.39
Normalized curvature vs. normalize depth for 6 ft. diameter shaft
193

LIST OF TABLES
2.1 
Peak response values for F=300 kips–Influence of soil-spring spacing
13
2.2 
Influence of ultimate soil resistance
15
2.3 
Influence of soil stiffness
16
2.4 
Fixed-base cantilever column study
17
2.5 
Effect of soil at large depth
18
2.6 
Effect of additional moment due to applied lateral load on top of shaft/column
19
3.1 
Analysis results: API p-y curves
38
3.2 
Analysis results: Experimental p-y curves
41
3.3 
Experimental results: Forces and displacements
43
3.4 
Summary: Analytical and experimental results
45
4.1  
API cyclic p-y analysis: Summary results .
65
4.2 
Experimental cyclic p-y analysis: Summary results .
66
4.3 
Cyclic p-y analyses: Curvature summary
68
4.4 
Gap model – 20% Drag: Summary results
88
4.5 
Gap model – 50% Drag: Summary results.
89
4.6 
Gap model – 80% Drag: Summary results.
91
4.7 
Analysis summary – Gap models 
92

4.8 
Ground line displacement: Summary results.
94

4.9 
Shaft/column curvature: Summary results.
95

5.1 
2 ft shaft/column: Summary results
125

5.2 
Analysis summary: Gap models
127

6.1
Summary of classification test results
145

6.2
Summary of consolidation test results
145

6.3
Summary of UU triaxial test results on clayey soils
148

6.4
E values based on consolidation data
152

6.5
E values based on PMT curves
152

6.6
E values obtained from shear wave velocities
152

6.7
Soil modulus values used for ABAQUS simulations
153

6.8
Value of E for moment-curvature relationship shown in Fig. 6.9
160

7.1
Slopes of p-y curves for initial linear section
190

LIST OF SYMBOLS

Chapters 1 to 5:

A 
factor to account for static or cyclic loading, when deriving p-y curves according to API (1993) recommendations

Ae 
effective shear area of column or beams

Ag 
gross area of the section (concrete and steel)

Ast 
total area of column reinforcement in the section

B
pile diameter

c 
undrained shear strength for undisturbed clay soil samples, psi (kPa),

cv                     coefficient of consolidation  
C 
cyclic loading coefficient defined by Eq. 3.3

Cd 
ratio of the maximum drag force to the ultimate resistance of the p-y element

Cr 
ratio of the maximum elastic force to the ultimate resistance of the p-y element

CPT
cone penetration test

D
shaft diameter

Ec
average modulus of elasticity of concrete

Epy 
subgrade reaction modulus of p-y curve

Es 
soil elastic modulus

EI
flexural stiffness of compression member

Fy_ API
load at yield displacement for analytical model using API p-y curves

F1/2y_ API 
load at half yield displacement for analytical model using API p-y curves

F2y_ API 
load at twice yield displacement for analytical model using API p-y curves 

Fy_ EXP
load at yield displacement for analytical model using experimental p-y curves

F1/2y_ EXP 
load at half yield displacement for analytical model using experimental p-y curves

F2y_ EXP 
load at twice yield displacement for analytical model using experimental p-y curves 

Fy_ TEST
load at yield displacement from test results

F1/2y_ TEST 
load at half yield displacement from test results

F2y_ TEST 
load at twice yield displacement from test results

F
lateral force applied at top of shaft/column

f’c 
average concrete compressive strength 

fsp 
average tensile strength determined from splitting tests 

fy
reinforcement yield strength 

Fr: 
average concrete tensile strength

h
current passive wedge depth (SW method)

H
pile depth below ground 

I
moment of inertia of section

Ic 
soil behavior type index (Robertson, 1990)

J 
dimensional empirical constant with values ranging from 0.25 to 0.5 (determined by field-testing), 

K 
initial modulus of subgrade reaction

Kc: 
closure tangent modulus

Kd: 
drag tangent modulus

Ke: 
elastic tangent modulus

Kp: 
plastic secant tangent

kT
constant that accounts for the variation of soil modulus with depth(z) (Terzaghi, 1955)

LL
liquid limit

lp 
plastic hinge length

M
bending moment

N
number of cylces

p 
actual soil lateral resistance, psi (kPa) 

pp 
pressure due to plastic pressure

pc 
pressure associated with closure

pd 
pressure due to drag force

pod 
pd at the start of the current loading cycle

Pe 
axial compressive force on the column

PL 
plastic limit

P0 
axial load capacity of the shaft/column 

pult
ultimate resistance, psi (kPa) 


[image: image1.wmf]*

L

P

 
ultimate pressure from pressuremeter test

qu
soil bearing capacity

s
slope

Su
soil undrained shear strength

T                     time factor for soil consolidation

V
shear

Vs                     shear wave velocity

X
depth below soil surface.

XR 
depth below soil surface to bottom of reduced resistance zone 

y 
actual lateral SHAFT deflection, in. (mm)

y50 
deflection under short term static load at one-half the ultimate resistance

yc 
deflection under N-cycles of load 

ye 
shaft displacement associated with elastic deformation

yg 
shaft displacement associated with gap deformation. 

yo+
memory term for the positive side of the gap

yo-
memory term for the negative side of the gap

yog
yg at the start of the current loading cycle

yp 
shaft displacement associated with plastic deformation 

ys 
deflection under short term static load 

W 
 unit weight of the reinforced concrete

z
depth below ground line

( y_ API
yield displacement at top of shaft/column for analytical model using API p-y curves

(1/2 y_ API
half yield displacement at top of shaft/column for analytical model using API p-y curves

 (2 y_ API 
twice yield displacement at top of shaft/column for analytical model using API p-y curves

( y_ EXP
yield displacement at top of shaft/column for analytical model using experimentally derived p-y curves

(1/2 y_EXP 
half yield displacement at top of shaft/column for analytical model using experimentally derived p-y curves

(2 y_ EXP 
twice yield displacement at top of shaft/column for analytical model using experimentally derived p-y curves

( y_ TEST 
yield displacement at top of shaft/column for test results

(1/2 y_ TEST 
half yield displacement at top of shaft/column for test results

 (2 y_ TEST 
twice yield displacement at top of shaft/column for test results

∆top 
displacement at top of shaft/column

∆ground
displacement at ground line

(C 
compressive strain

(T 
tensile strain

(c 
strain which occurs at one-half the maximum stress on laboratory undrained compression tests of undisturbed soil samples

(
effective unit weight of soil, lb/in.3 (MN/m3)

(s 
shear wave velocity

(p 
P-wave velocity

· mass density of the soil 

(longitudinal:
longitudinal steel ration 

(transversal: 
transversal steel ration


angle of internal friction for soil

(
curvature

(max_test
maximum curvature based on test results

(max_API
maximum curvature based on analytical results, using API p-y curves

(max_EXP
maximum curvature based on test results analytical results, using experimentally derived p-y curves

(m
mobilized effective stress friction angle of the soil (SW method)

Chapters 6 and 7

c   
soil cohesion intercept


[image: image2.wmf]v

c


coefficient of consolidation for soil

Cc
soil compression index

Cr 
soil swell index

D
soil constrained modulus 

e  
void ratio for soil

fs
sleeve resistance in seismic cone penetration test

G
shear modulus for soil

Gmax
maximum shear modulus for soil

Hdr
length of drainage path for soil

E0
 soil  initial elastic modulus 

E+
soil elastic modulus in compression

E-
 soil elastic modulus in tension

EI
flexural stiffness of compression member

M
bending moment

Pa
atmospheric pressure


[image: image3.wmf]*

L

P


ultimate pressure from pressuremeter test

qc
tip resistance in seismic cone penetration test

Rf
friction ratio in seismic cone penetration test

R0
the initial probe radius in pressuremeter test

S    
degree of saturation for soil

Su
soil undrained shear strength

T 
time factor in soil consolidation test

U 
average degree of consolidation

Vs   
shear wave velocity for soil

y        
lateral displacement of a deformed shaft    


[image: image4.wmf]'

i

y

       
slope of a deformed shaft

σvo
soil overburden stress


[image: image5.wmf]vo

'

s


soil effective overburden stress


[image: image6.wmf]'

p

s


soil preconsolidation pressure

∆R
the probe radius change in pressuremeter test

Δσv
change of overburden pressure in consolidation test

∆σdf
deviator stress at failure in UU triaxial test

σult
ultimate deviator stress in UU triaxial test

εf 
soil failure strain in UU triaxial test

ε50
50% of soil failure strain

   
soil unit weight

  
soil Poisson’s ratio 

  
angle of internal friction (in degrees) for soil

 
dilation angle (in degrees) for soil


soil density


[image: image7.wmf]f

   
curvature 

ACKNOWLEDGMENTS

Support for this research was provided by the California Department of Transportation under Research Contract No. 59A0183 (A01), which is gratefully acknowledged. We would like to acknowledge the valuable assistance and technical support of Caltrans staff in this project, particularly Mr. Anoosh Shamsabadi and Mr. Craig Whitten. Mr. Sahan Abeln and Mr. Kutay Orakcal of UCLA, and Dr. Frank McKenna and Michael Scott of UC Berkeley, are thanked for their assistance with the development and implementation of the OpenSees gap model, respectively. Dr. Silvia Mazzoni, former post-doctoral researcher and lecturer at UCLA, is acknowledged for her help with the use of OpenSees.  

EXECUTIVE SUMMARY

Cast-in-drilled-hole (CIDH) bridge shaft/columns provide an economical option for California highway construction. The inelastic deformations for a CIDH shaft/column occur below grade; therefore, the overall lateral load behavior of the system is influenced by the interaction between the shaft and the surrounding soil, commonly modeled using p-y curves. Current models for p-y curves are calibrated primarily from lateral load testing of relatively small diameter shafts and pile. This study utilizes test results of a full-scale, 6 ft (1.8 m) diameter, reinforced concrete shaft/column that was constructed and tested to failure under cyclic lateral loading. Details of the testing program are provided in Part I of this report. Part II is concerned with analytical studies and modeling associated with the project. Research findings are presented in two subsections. First, results obtained using the p-y model studies are presented in Chapters 2-5, followed by the findings obtained in the three-dimensional finite element modeling studies in Chapters 6 and 7.

The p-y model studies utilized a two-dimensional nonlinear finite element model of the test specimen. The shaft/column was modeled using a flexibility-based fiber model. The soil around the shaft was modeled using two types of p-y models, one in which the nonlinear soil-shaft interaction is modeled using a nonlinear spring, and a second that includes a gap element model. Analyses utilizing p-y springs developed from the API design guidelines predict a softer load-displacement response than that obtained from experiment. Analyses performed using models of p-y curves derived from the experimental test results capture reasonably well the load-displacement response of the test shaft. However, the best results are obtained when the experimental p-y model is modified to allow for gapping and drag effects. 

A 3-D finite element model (ABAQUS) was used to provide numerical simulations of the laterally-loaded 6 ft. diameter shaft. The soil-shaft contact, elastic/plastic constitutive behavior of soil, and nonlinear behavior of reinforced concrete were simulated. Effect of shaft diameter on the results of numerical simulations was studied comparing the results from 2 ft. and 6 ft. diameter shafts simulations. Results showed good agreement between simulations and field measurements for lateral load vs. lateral displacement at the top of the shaft, p-y curves at various depths, and shaft curvature vs. depth. Results also showed that gap width at the ground surface, gap depth, and hinge point depth increase with increasing applied load. It was also found that cyclic lateral loading produces a larger gap around the shaft than static lateral loading. Simulation results indicated that shaft diameter has an important effect on the slope of the initial linear section of a p-y curve. 

PAGE  

iii



_1072032564.unknown

_1072201633.unknown

_1072092634.unknown

_1064648059.unknown

_1072032010.unknown

_1064646551.unknown

